SPECIFICATION

Section 07900

Wabo®StripSeal Armored Edge

Expansion Joint System

PART 1 - GENERAL

1.01	Work Included

A.	The work shall consist of furnishing and installing expansion joints in accordance with the details shown on the plans and the requirements of the specifications. The joints are proprietary designs utilizing extruded elastomeric seals, engineered steel embedment shapes and elastomeric concrete headers.

B.	Related Work

- Cast-in-place concrete

- Miscellaneous and ornamental metals

- Flashing and sheet metal

- Sealants and caulking

1.02	Submittals

A.	Template Drawings - Submit typical seismic joint cross-section(s) indicating pertinent dimensioning, general construction, component connections, and anchorage methods.

1.03	Product Delivery, Storage and Handling

- Deliver products in each manufacturer's original, intact, labeled containers, pallets or bundles and store under cover in a dry location until installed. Store off the ground; protect elastomeric header material’s pre-mixed components from weather and construction activities.

1.04	Acceptable Manufacturers

A.	All joints shall be as manufactured/supplied by 25 Bridle Lane, Westborough, MA 01581 USA

B.	Alternate manufacturers and their products will be considered, provided they meet the design concept and are produced of materials that are equal to or superior to those called for in the base product specification.

- Any proposed alternate systems must be submitted and receive approval 21 days prior to the bid. All post bid submissions will not be considered. This submission shall be in accordance with MATERIALS AND SUBSTITIONS.

- Any manufacture wishing to submit for prior approval must provide the following:

- A working 6 inch sample of the proposed system with a letter describing how the system is considered superior to the specified system.

- A project proposal drawing illustrating the recommended alternate system installed in the application, specific to the project.

- Verifiable list of prior installations showing prior and successful experience with the proposed system.

- Any substitution products not adhering to all specification requirements within, will not be considered.

1.05	Quality Assurance

A.	Warranty: Standard material limited warranty or project specific warranty available. Installation shall be in strict accordance with manufacturer’s technical specifications, details, installation instructions and general procedures in effect for normal intended usage and suitable applications under specific design movements and loading conditions.

B.	Manufacturer: Shall have a minimum ten (10) years experience specializing in the design and manufacture of parking expansion control systems.

C.	Products: Expansion control systems shall be installed with manufacturer’s blockout repair materials.

E.	Application: Minimum 2 years [documented] experience in work of this Section.

PART 2  -  PRODUCT

2.01	General

A.	Provide watertight expansion control system that is capable of accommodating multi-directional movement. System shall consist of heavy duty extruded or machined steel shapes cast into the structure by means of sinusoidal anchorage and a field mixed elastomeric concrete header material. The steel shapes shall be designed to accept and mechanically lock manufacturer’s elastomeric seal. Provide optional seal profiles that satisfy project requirements including movement. Where required, utilize manufacturer’s seal profile that complies with ADA guidelines and accepts pedestrian traffic.

Furnish Wabo®StripSeal System, Model “SSS” for horizontal locations requiring watertightness as supplied by Sika Emseal and as indicated on drawings.

2.02	Components and Materials

- Steel Extrusions and Shapes - Material to conform to properties of ASTM  A36 (shapes). Profile shall be heavy duty and capable of accommodating various horizontal conditions and service load requirements including HS-20 loading. Design profile with semi-closed cavity and features that will provide a mechanical lock for the Elastomeric Seal. Provide shapes as detailed on contract drawings. Hot or cold rolled shapes exhibiting hollow tube like centers and/or open bottom seal lug cavities will not be permitted.

B.	Sinusoidal Anchorage - Provide manufacturer’s preformed sinusoidal steel profile.  Material shall be a minimum 3/8” diameter and meet the requirements of ASTM A36.

C.	Elastomeric Seals - Material shall typically be a flexible, extruded compound exhibiting the physical properties listed in the table below. Utilize manufacturer’s alternate materials and seal profiles selected from their standard product offering to meet the requirements of product application. All seals shall incorporate a unique locking lug that mechanically snaps into a corresponding extrusion or machined shape cavity to ensure watertightness and proper joint performance. Where required, provide manufacturer’s seal profile that complies with ADA guidelines and accepts pedestrian traffic.

- PHYSICAL PROPERTIES OF POLYCHLOROPRENE (NEOPRENE) SEAL ELEMENT

All Model Series Profiles (Except “SEC” Series)

| Physical Properties | ASTM Test Method | Requirements |
| --- | --- | --- |
| Tensile Strength, min. | D-412 | 2000 psi |
| Elongation @ break min. | D-412 | 250% |
| Hardness, Type A Durometer | D-2240 (Modified) | (55 +/-5) |
| Compression set. | D-395, Method B | 40% |
| 70 hr. @ 212°F max. | (Modified) |  |
| Oven Aging, 70 hr. @ 212°F | D-573 |  |
| Tensile strength, loss, max. |  | 20% |
| Elongation, loss, max. |  | 20% |
| Hardness, Type A. Durometer |  |  |
| (points change) |  | 0 to +10 |
| Oil Swell, ASTM oil 3, 70 hr. |  |  |
| @ 212°F weight change, max. |  | 45% |
| Ozone resistance | D-1149 |  |
| 20% strain, 300 pphm, in air |  |  |
| @ 104°F (wiped with Toluene |  |  |
| to remove contamination). |  | No Cracks |

2.	PHYSICAL PROPERTIES OF THERMOPLASTIC RUBBER SEAL ELEMENT

Model Type “SEC-250 or 400”  Series Profile

| Physical Properties | ASTM Test Method | Requirements |
| --- | --- | --- |
| Material |  | Thermoplastic rubber |
| Hardness | D-2240 | 67A ± 3 |
| Specific Gravity | D-792 | 0.97 ± 2 |
| Tensile Strength | D-412 | 1050 psi |
| Ultimate Elongation | D-412 | 410% |
| 100% Modulus | D-412 | 420 psi |
| Tear Strength | D-624 | 140 lb/in |
| Tension Set | D-412 | 10% |
| Compression Set | D-395 | 23% @ 77°F |
| 168 hrs. |  | 36% @ 212°F |
| Brittle Point | D-746 | -81°F |

D.	Lubricant Adhesive - Prima-Lub Adhesive (as recommended by the joint manufacturer) shall be a one part moisture curing polyurethane and aromatic hydrocarbon solvent mixture which complies with ASTM D-4070.

E.	Elastomeric Concrete - (Wabo®Crete Parking Series)

Material shall be an ambient cure, 100% solids, two component polyurethane with pregraded aggregate mix exhibiting the physical properties listed in the tables below.  When properly mixed and poured, the elastomeric concrete cures rapidly, flows and fills any voids, spalls or irregularities forming a monolithic unit.

1.  Elastomeric cured binder and aggregate shall meet the following physical properties:

PHYSICAL PROPERTIES      ASTM METHOD       REQUIREMENTS          TEST RESULTS

Compressive Strength             D695 Mod                    2200                             2723 psi

Resilience at 5% deflection      D695                             90 (min.)                         96.7%

Adhesion to concrete:              C190

Dry Bond                                                  400                              451.3 psi

Wet Bond                                                  250                             353.9 psi

Impact Resistance                  Steel ball drop (.375” th. Disc / dry steel plate)

At  -20 deg F(-29C)                                         no cracks at 5 ft                7.0 ft-lbs

At   32 deg F (0C)                                            no cracks at 5 ft              10.0 ft-lbs

At 158 deg F (70C)                                          no cracks at 5 ft              10.0 ft-lbs

F.	Bonding Agent

Provide manufacturer’s two component, 100 percent solids bonding agent and apply to the sides and base of the preformed concrete blockouts prior to placement of Wabocrete® elastomeric concrete header. Store, mix and apply in accordance with manufacturers system data sheet.

Liquids components shall be identified by the following information:

Part A - Resin       -	Color:  Clear

Part B - Activator -	Color:  Black

G.	Accessories - Provide necessary and related system components including leveling devices and optional aggregate for elastomeric concrete which is utilized to enhance non-slip, UV resistance and aesthetic appeal of the final installation. (Refer to installation procedures)

2.03	Fabrication

A.	Steel extrusions and shapes to be shipped in manufacturer’s standard lengths (typically 20 ft) and shall be cut to exact length on jobsite where required. Extrusions shall be miter cut in the field to conform to directional changes unless otherwise contracted with expansion joint manufacturer to provide factory manufactured transitions.

B.	Sinusoidal anchorage profiles shall be shop welded to the steel extrusions and shapes in accordance with manufacturer’s drawings.

C.	Elastomeric seals shall be shipped in the longest practical continuous length in manufacturer’s standard shipping carton or on wooden pallets shrink-wrapped.  Miter cut in the field to conform to directional changes unless otherwise contracted with expansion joint manufacturer to provide factory manufactured transitions.

D.	Elastomeric concrete components shall be shipped in manufacturer’s approved containers on wooden pallets shrink-wrapped.

2.04	Finishes

A.	If not specified hot dipped galvanized by engineer or owner steel extrusions and shapes shall be supplied in standard mill finish. All seal cavities shall receive manufacturer’s standard coating for protection from rusting prior to shipping.

B.	If specified by engineer or owner ASTM A36 steel extrusions and shapes shall be hot dipped galvanized in accordance with ASTM  A-123 if specified by engineer.

C.	Elastomeric seals shall be supplied in standard color:  Black.

- Elastomeric concrete header material:

- Elastomeric Header base material shall be supplied in standard color: Gray.

- Elastomeric Header material after field application of optional broadcast aggregate granules.

PART 3 - EXECUTION

3.01	Installation

A.	Protect all expansion joint component parts from damage during placement of work in adjacent areas, construction traffic and thereafter until completion of structure.

- Expansion joint systems shall be set to the proper width for the ambient temperature at the time of installation. Properly align all steel extrusions and shapes prior to field welding operations to ensure proper joint performance and watertightness. This information is indicated in the contract plans.

C.	Expansion joint systems shall be installed in strict accordance with manufacturer's written installation instructions along with the advice of their qualified representative. Contact manufacturer to discuss field splicing of all profiles and components prior to their installation to verify correct and proper procedures. Ends of steel extrusions and shapes shall be prepared by contractor for field welding butt splices along rail lengths to ensure watertightness following manufacturer’s standard weld details.

3.02	Clean and Protect

A.	Protect expansion joint system during construction. Heavy construction vehicles will not be permitted to cross the joint without specific and written permission by the Engineer. Subsequent damage to the system shall be repaired at the contractor’s expense.